**Spectrum details**

Project New project Spectrum name Spectrum 1

**Electron Image**


Image Width: 49.2 µm



**Acquisition conditions**

Acquisition time (s) 100.0 Process time 5

Accelerating voltage (kV) 15.0



**Quantification Settings**

Quantification method All elements (normalised)

Coating element None

**Summary results**

|  |  |  |  |
| --- | --- | --- | --- |
| Element | Weight % | Weight % σ | Atomic % |
| Silicon | 24.284 | 0.087 | 35.358 |
| Titanium | 75.716 | 0.087 | 64.642 |