Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  50.0 	Process time  4

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 8.368 | 2.174 | 37.043 |
| Tantalum | 91.632 | 2.174 | 62.957 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  50.0 	Process time  4

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 17.378 | 2.092 | 57.539 |
| Tantalum | 82.622 | 2.092 | 42.461 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  50.0 	Process time  4

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 22.407 | 2.301 | 65.041 |
| Tantalum | 77.593 | 2.301 | 34.959 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 98.4 µm

Acquisition conditions

Acquisition time (s)  50.0 	Process time  4

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 16.544 | 2.116 | 56.085 |
| Tantalum | 83.456 | 2.116 | 43.915 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 655.9 µm

Acquisition conditions

Acquisition time (s)  49.8 	Process time  4

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 11.333 | 2.076 | 45.160 |
| Tantalum | 88.667 | 2.076 | 54.840 |