Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  50.3 	Process time  4

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 37.869 | 0.411 | 50.968 |
| Titanium | 62.131 | 0.411 | 49.032 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  50.0 	Process time  4

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 50.316 | 0.448 | 63.332 |
| Titanium | 49.684 | 0.448 | 36.668 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  50.0 	Process time  4

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 36.945 | 0.421 | 49.982 |
| Titanium | 63.055 | 0.421 | 50.019 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 4

Electron Image

Image Width: 196.8 µm

Acquisition conditions

Acquisition time (s)  50.0 	Process time  4

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 33.557 | 0.421 | 46.275 |
| Titanium | 66.443 | 0.421 | 53.725 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 1.968 mm

Acquisition conditions

Acquisition time (s)  50.2 	Process time  4

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 36.513 | 0.441 | 49.517 |
| Titanium | 63.487 | 0.441 | 50.483 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 1

Electron Image

Image Width: 109.3 µm

Acquisition conditions

Acquisition time (s)  50.0 	Process time  4

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 50.818 | 0.488 | 63.797 |
| Titanium | 49.182 | 0.488 | 36.203 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 2

Electron Image

Image Width: 109.3 µm

Acquisition conditions

Acquisition time (s)  50.0 	Process time  4

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 37.532 | 0.458 | 50.610 |
| Titanium | 62.468 | 0.458 | 49.390 |

Spectrum details

Project	New project 	Spectrum name	Spectrum 3

Electron Image

Image Width: 109.3 µm

Acquisition conditions

Acquisition time (s)  50.0 	Process time  4

Accelerating voltage (kV)	15.0

Quantification Settings

Quantification method	All elements (normalised)

Coating element	None

Summary results

| Element | Weight % | Weight % σ | Atomic % |
| --- | --- | --- | --- |
| Silicon | 32.843 | 0.444 | 45.476 |
| Titanium | 67.157 | 0.444 | 54.524 |